LulzBot Filament Testing Report

Manufacturer: Formfutura
Filament Type: PVA	/ AquaSolve
Tested By:	Ben Baldwin
Test Date(s):	6/5/17-6/16-17

Ease of use:	5/10
Appearance:	8/10
Color consistency:	8/10
Print temperature Range (C): 195-200°C
Manufacturers recommended: 190°C-210°C
Variance in diameter: (2.84-2.91mm)
Minimum bend radius: 50mm
Prints using current Lulzbot profiles/temps: esun PVA temp up to 195-200°C
Decomposition Temperature: >210°C

General Notes:	(Be as detailed as possible)
- Do not print above 210°C
- bag not well vacuum sealed
- desiccant packet wrapped into spool seems to cause uneven drying of filament
- Good looking packaging
- very hard filament brittle in many spots

Recommended Print Profiles: (ie. should we include high clarity, high strength, etc.)

Health or environmental risks:

Disposal Options:

Per SDS: Generation of waste should be minimized, check possibility for recycling. Waste product can be incinerated or dumped together with domestic waste in compliance with local authority requirements.

Recommendation:	(As thorough as possible)

I do not recommend this PVA although it is very consistent in color and diameter variance the material is brittle in places. For this reason it is easy to snap and strip out. The material generally did not stick well to other materials (various PLA’s). Also being a higher temperature material makes it more likely to cause jams if idled in the hot-end for long periods of time.

Experience based on cura2 alpha testing with v3 dual proof of concept prototypes.

Revision History

Revision Date	Modifications or Additions	Updated By
04.24.17	Creation of AquaSolve filament testing document.	JTP
6/26/2017	Fill out test report.	BJB