LulzBot Filament Testing Report

Manufacturer:	Functionalize
Filament Name:	PLA 3mm Black conductive
Filament Type:	F-Electric
Tested By:	Patrick R.
Date:	02/16/2016

Ease of use:	8/10
Appearance:	9/10
Color consistency:	10/10
Print temperature Range (C):	200-230/50-60
Variance in diameter: (2.86-2.86)
Minimum bend radius: Filament breaks very easily.
Prints using current Lulzbot profiles/temps: Default conductive profile works great.

General Notes:
- Manufacturer recommended printing range 215C to 230C (215 wielded better results for me).
- Filament is extremely brittle need to make sure there are no sharp bends to avoid snapping.
- Color was consistent throughout reel.
- Nice professional looking packaging and reel.
- It was it measured around the same resistivity as our current conductive filament.
- Best part about this filament is that it does not require extra purging to clean out and does not leave a residue on the pei like the protopasta filament.
Health or environmental risks:
May cause eye irritation, May cause respiratory irritation, if sanding, if swallowed seek immediate medical attention.
Disposal Options:
Do not dispose of down drain. Do not create dust when cleaning up, use water sprayer if necessary.

Recommendation:
It might be a little more expensive, and a little more brittle but has some real positives to it prints with default conductive profile, does not leave residue on pei, and it purges out of the nozzle easily.

Illustration 1: Functionalize

Illustration 2: Protopasta