LulzBot Filament Testing Report

Manufacturer: Ninjaflex
Filament Type: Semiflex
Tested By:	Mike Rosenhagen
Date:	10/3/17

Ease of use:	6/10	I had trouble feeding the filament down into the tool head and it won’t extrude consistantly.
Appearance:	9/10
Color consistency:	10/10
Print temperature Range (C):	(230-240C/40-60C)
Variance in diameter: (2.83-2.88)
Minimum bend radius: N/A
Prints using current Lulzbot profiles/temps:

General Notes:	(Be as detailed as possible)
- Need to put a little glue on bed
- Seems to get clogged/stuck occasionally

Recommended Print Profiles: (ie. should we include high clarity, high strength, etc.)

Health or environmental risks:

Disposal Options:

Recommendation:	(As thorough as possible)

Revision History

Revision Date	Modifications or Additions	Updated By