LulzBot Filament Testing Report

Manufacturer:	Village Plastics
Filament Name:	PLA 3mm Sparkly Blue
Filament Type:	PLA
Tested By:	Patrick R.
Date:	02/15/2016

Ease of use:	8/10
Appearance:	9/10
Color consistency:	10/10
Print temperature Range (C):	180-230/50-60
Variance in diameter: (2.86-2.88)
Minimum bend radius: 10-20mm the pla is a little more brittle than some of the other village pla's.
Prints using current Lulzbot profiles/temps: Default pla profile will print with limited success, but for an optimal print I would recommend creating a new profile with higher temperature settings.

General Notes:
- Would need to create a new profile with higher temperatures to get acceptable print quality.
- Has an ugly murky finish to print when temperature is to low.
- Color was very consistent throughout the roll.
- Nice professional looking packaging and rolls like other village filaments.
- The material is a little brittle but not enough to snap during printing.
Health or environmental risks:
Contact with eyes, and skin may cause irritation, ingestion may cause irritation and vomiting. inhalation of dust may cause sore throat and couch but is considered a low hazard risk.

Disposal Options:
Do not flush into surface water or sanitary sewer system.

Recommendation:
Its cool looking fun new filament I think people would buy it. It would require some extra work on our end since default pla profiles do not work well enough to make acceptable prints with this filament.

Illustration 1: Printed at 210C with increased z acceleration to 500