LulzBot Filament Testing Report

Manufacturer:	TwoBEars
Filament Type:	Silk
Tested By:	Patrick
Date:	4/29/2016

Ease of use:	8/10
Appearance:	10/10
Color consistency:	10/10
Print temperature Range (C):	180-200 C
Material Physical Properties:
Melting point / range: 140-200°C
Ignition temperature: not tested
Decomposition temperature: 205-210°C
Variance in diameter: (2.78-2.93)
Minimum bend radius: This filament is really bendy couldnt get it to break.
Prints using current Lulzbot profiles/temps:
A new profile would need to be created for this filament it doesnt print well at pla temperatures. Changed temp to 180 and increased min layer time to 25-30 and turned fan on full at 3 mm to get good results.

General Notes:
- Parts have a really cool shiny finish to them.
- Prints great at a low temperature.
- Color consistent throughout the roll.
- Nice professional looking packaging.
- I think they accidently stamped the wrong exp. Date on this reel.

Health or environmental risks:

Under normal conditions the processing and compounding is stable and there are no observable
hazardous reactions nor products of decomposition.
No toxicologic short-term or long-term effects are known.
The material is only composed of eco-friendly components. So the material can be count as eco-friendly.

Disposal Options:

The best way of disposal is
I.) Recycling, i.e. recovery of the material or
II.) brun, with due regard to the local laws and regulations

Recommendation:
I highly recommend we sell this filament the prints look great and its a specialty filament that cant really be compared to anything else.