LulzBot Filament Testing Report

Manufacturer: CC Products
Filament Type: High-T-Lay
Tested By:
Date:

Ease of use:	3/10
Appearance:	5/10
Color consistency:	5/10
Print temperature Range (C):	(235°C-245°C)
Variance in diameter: (2.65mm-2.67mm)
Minimum bend radius: 25mm
Prints using current Lulzbot profiles/temps:

General Notes:	(Be as detailed as possible)
- http://lay-filaments.com/portfolio-item/high-t-lay
- Print Temperature listed on site is ~ up to 240°C which seems high (test to determine actual temp)
- Material is intended to be a support material dis-solvable by water
- Thermal Decomposition > 255°C, do not print above this temperature
- Very Brittle
- Color is very inconsistent
- Diameter is very small for 3mm

Recommended Print Profiles: (ie. should we include high clarity, high strength, etc.)

Health or environmental risks:

Disposal Options:
Small amounts can be incinerated or dumped together with domestic waste
(in compliance with local authority requirements).

Recommendation:
Don’t use. Because the diameter is too small for 2.85mm the bead was severely under extruded. Also, with it coming in a coil, I was unable print without tending the coil by rotating the every so often.
If extruded to proper size and and wound on a spool I believe it would do much better.

Revision History

Revision Date	Modifications or Additions	Updated By
04.27.17	Created initial document	J. Pettit