LulzBot Filament Testing Report

Manufacturer: Chromastrand
Filament Type: High Impact Grade ABS
Tested By:	bam
Date:	04/30/2017

Ease of use:	8/10
Appearance:	10/10
Color consistency:	10/10
Print temperature Range (C):	(220-250/105-110)
Variance in diameter: (2.80-2.86)
Minimum bend radius: NA
Prints using current Lulzbot profiles/temps: Yes, great w/ Village Plastics ABS profiles

General Notes:
- This ABS prints very well with standard ABS settings
- Great color consistency.
- This ABS seems to need the 105-110C bed temperature in order to stay stuck to the bed.
- This is the same ABS blend that we have been testing and have approved for use in the cluster with few profile changes, it can be treated as a direct replacement for Village plastics ABS.
- The filament has 8/10 for ease of use only because of the issues inherent in all most ABS including warping, splitting and a high required bed temperature.

Recommended Print Profiles: Just the standard 3 should be fine. If anything we could include a “production part” profile similar in layer height, infill and speeds to what we use for structural parts in the printers.

Health or environmental risks:

As typical with ABS, good general ventilation is recommended.

Disposal Options:
Do not dump into any sewers, on the ground or to any body of water. All disposal methods must be in compliance with all Federal, State and local laws and regulations. Check with local authorities.

Recommendation:
This is a great ABS, and is a good replacement for Village Plastics ABS both for cluster use and retail. Chromastrand’s use of top of the line colorants and the higher heat deflection temperature make this a nice premium material for structural parts that need good heat resistance.
Revision History

Revision Date	Modifications or Additions	Updated By
04.17.17	Initial Document Creation	J. Pettit
04.30.17	Filament testing notes added	bam