LulzBot Filament Testing Report

Manufacturer:	3DOM USA
Filament Name:	Wound Up
Filament Type:	Coffee filled PLA
Tested By:	Brent M
Date:	9/15/15

Ease of use:	10/10 – prints just like regular PLA
Appearance:	9/10
Size consistency:	Good
Color consistency:	Good
Print temperature:	200-205C / 60C
Prints using Lulzbot profiles/temps: Yes, using standard PLA profiles

Recommendation: This is a pretty fun filament that smells a bit like coffee while printing, and a LOT like coffee when opening the bag (it contains a coffee pouch). Printed parts have great color and surface finish, a nice translucent brown PLA, finished parts do not smell noticeably like coffee when cool. It's a fun filament to print with, and definitely “Lulzbot Approved”.

Notes:
- Nice sweet coffee smell when printing
- Seems to be more of a dyed PLA than a filled PLA
- Prints well with standard PLA settings, for a default profile for this material I would drop extrusion temp to 200C, no other changes seem to be needed.
- Finished parts do not smell like anything really.
- Filament came packaged nicely in a branded box complete with a real quality report on the mean diameter, ovality and production date. Nice!
Filament	Variance in diameter	Maximum out of round	Extrusion temperature
“Wound Up” Coffee PLA	2.77-2.84mm (2.805mm AVG) / 0.07mm variance	2.80-2.83 (0.03mm ovality)	190-210C range / 200C / 60C ideal