LulzBot Filament Testing Report

Manufacturer:	Taulman
Filament Name:	Nylon 910 filament 3.00mm
Filament Type:	FDA Thermal Nylon
Tested By:	Patrick
Initial Date:	3/18/2015
Updated:	07.18.16

Ease of use:	8/10
Appearance:	Clear Frosty
Size consistency:	Average
Color consistency:	Good
Print temperature:	235/100
Bed adhesion:	Gluestick
Prints using Lulzbot profiles/temps: Yes, maybe tweak temperature up in bridge profile

Recommendation: This filament seems awesome. It doesn’t bubble like most of the nylons do when printing at temperatures past 250C. Being able to print this at a higher temperature means the parts come out more solid than some of the other nylons which sometimes suffer from layer splitting. It has a high variance in diameter which is the case with many nylons but I didn't run into any problems when printing it.

Notes:
- Can print the existing bridge profile, recommend upping the temperature though
- Will not bubble/boil until you get to 280C
- Prints are very solid printing at the higher temperature
- The variance in diameter was sub-par
- Black 910 tested in July of 2016 appears to have the same results as the natural initially evaluated
Filament	Variance in diameter	Maximum out of round	Extrusion temperature
3mm FDA Thermal Nylon	2.88-3.06 (.18mm)	0.21mm (3.04-3.06)	210-270C (printed at 240C with modified bridge Mini profile)

Revision History

Revision Date	Modifications or Additions	Updated By

07.18.16	Added information regarding Black 910	J. Pettit