Lulzbot Filament Testing Report
Manufacturer: Taulman
Filament Type: Alloy 960 Carbon Fiber
Colors Tested: Natural on label, filament looks Black
Tested By: Angie Suiter
Date Started: 11/14/2018
Date Completed: N/A

Printer Data
Bed Surface/Covering: Heated bed with PEI
Toolhead Types Used: Hardened Steel Plus and Hardened Steel
Printer Type: Mini 2
Wiper Pad Type: x2 coated ABS
Other Notes: ---

Manufacturer Recommended Settings
Print Temp: 270-280 C
Bed Temp: 65-75 C
Fan Speeds:
Printing Speeds: (HS = 30mm/s)(HS+ = >22mm/s)
Other:

Pre-Printing Filament Assessment
Basic Use Research:
-
-
-
-
-
Health or Environment Risk:
Disposal Options:
Other SDS Notes:
Packaging Notes:
Minimum Bend Radius:
Bend Test Notes: < 40 mm diameter round.
Bubble/Debris Test Results: This fill does not snap or break, it bends with minor deformation, I believe it would still be printable once deformed due to a sharp bend.
Color Consistency: No variance in color through reel.
Filament Diameter Variance: 0.14 mm varience
Average: 2.81 mm
Data Points: 2.83, 2.90, 2.80, 2.81, 2.83, 2.82, 2.85, 2.84, 2.80, 2.80, 2.80, 2.82, 2.86, 2.79,	2.85, 2.85, 2.81, 2.80, 2.79, 2.81, 2.82, 2.81, 2.79, 2.78, 2.81, 2.78, 2.81, 2.76, 2.81
Moisture Absorption: TEST SUSPENDED water in pellets created craters of air pockets inside the	filament after drying. Unable to print.
Min Extrusion Temp: ---
Max Extrusion Temp Before Boil: ---
Min Bed Sticking Temp: ---
Other Notes: ---

Run a Control Print with an Available Comparable Material Profile
Results:
Profile Used: PA-CF - Colorfabb

Recommended Profile Changes

Printing Filament Assessment
Bed Adhesion Notes: ---
Layer Adhesion Notes: ---
Overhang/Bridging Notes: ---
Color Consistency/Change: ---
Part Removal Notes: ---
Other Notes: ---

Profile Assessment and Base Setting Recommendations
Bed Temperature Range: ---
Printing Temperature Range: ---
Fan/Cooling Range: ---
Printing Speeds: ---
Other Notes: ---

Manufacturer Filament Revision Notes
Revision Reason:
Expected Change:
Date: