Taulman Filament testing notes:

Notes:
PCTPE
- Does not stick to the bed very well on PET with lulzjuice like most nylons, but will stick down with gluestick fairly well.
- Very low warping compared to other nylons
- Steam comes from the nozzle when it first starts extruding this filament.
Tritan
- This is super strong, and prints like t-glase
- Took a few tries to get temperature right for a good looking print.
- Sticks to bed pretty easily with glue or lulzjuice.

Tech G
- Sticks to the bed easily with or without glue and comes off with limited force.
- It is clearest filament that I've seen so far.

Bio G
It prints exactly like Tech G in every way that I could tell.
Recommendation: .

All of these filaments were impressive in their own ways, and I expect that we'll get on board with at least a few of them. The Tritan and the PCTPE were the standouts, with tritan printing like a slightly lower temperature, low warp polycarbonate. It's also optically clear like the natural t-glase.

PCTPE is fairly flexible, it will bend easily but doesn't stretch much at all. It sticks well to gluestick on PEI or PET, and has the major advantage of not warping much.

Filament diameter accuracy / consistency:

Filament	Variance in diameter	Maximum out of round	Extrusion temperature
PCTPE	1.76-1.82 (.6mm)	0.07mm (2.87-2.94)	225-230C (printed at 240C with .4mm hex nozzle)
Triton	1.71-1.83 (.11mm)	0.01mm (1.82-1.83)	270-280C (printed at 275C with .4mm hex nozzle)
Tech G	1.70-1.76 (.6mm)	0.01mm (1.75-1.76)	238-245C (printed at 245C with .4mm hex nozzle)
Bio G	1.71-1.76 (.5mm)	0.01mm (1.75-1.76)	238-245C (printed at 245C with .4mm hex nozzle)
Average	1.75mm (+/- .45mm)	0.025mm

From Left PCTPE, Bio G, Tech G, Tritan