LulzBot Filament Testing Report

Manufacturer:	Toner Plastics
Filament Name:	Black PLA 2.88mm, Lot # 76983
Filament Type:	Opaque black pla
Date:	1/4/2015

Ease of use:	9/10
Appearance:	Good, dull surface at standard Lulzbot print temps
Size consistency:	Good
Color consistency:	No variance
Print temperature:	205/60 (LulzBot Mini)
Prints using Lulzbot profiles/temps: Yes

Recommendation: This PLA prints great at our with our standard print profiles. Is very similar to their opaque red PLA, the extrusion consistency was good, but more recent samples of TP PLA are much more consistent.

Notes:
- Prints well using standard PLA settings
- Very little stringing
- Seems like it should be printed at a hotter temperature than our current PLA, but does fine at the default settings
Filament	Variance in diameter	Maximum out of round	Extrusion temperature
2.88mm PLA / Batch # 77274	2.86-2.93 (.07mm) / Note: More recent samples are better	0.04mm (2.87-2.91)	190-210C (printed at 205C with standard Mini profiles)