A2 hardened steel Lulzbot edition plated steel nozzle

Currently the Lulzbot edition hexagon nozzle has some known issues. We currently see RMAs for breaking and leaking most often. The nozzle is the usually the source of the problem. The nozzle is made from beryllium copper C17200. A2 hardened steel is significantly harder and has a much higher tensile strength than C17200 while maintaining good machinability. A2 steel nozzles were ordered for testing the nozzle in the pictures below are the result of destructive testing. The nozzle was threaded into a block with the purpose of torquing until the nozzle broke, as you can see, the nozzle did not break even after extreme torque was applied. The wrench used in the test deformed before the nozzle would break. The marring on the block in the picture shows that even under the immense torque this nozzle would still have a good seal with the block.

Results from intentional over torquing

Other problems include wear and print contamination. Many times a simple solution already exists, in our case the injection molding industry has solved this same problem with the molds wearing and contaminating early. Electroless nickel coatings and injection mold releases are a great way to prevent tool wear, so these steel nozzles were coated in Twincladxt which is a hardened coating with excellent wear characteristics and a very low coefficient of friction. This mold release also provides excellent surface uniformity(<2.5 microns). The low friction aided in prevention of probe fails during the wear characteristics test, while the hardness helped mitigate wear significantly.

problems with current rev
  - leaking
    - causes
      - breakage
      - sealing surface finish
    - possible solutions
      - higher grade material to prevent breakage
      - tighter tolerance machining
  - breaking
    - causes
      - poor grain structure
      - over tightening
      - low tensile strength
    - possible solutions
      - higher grade material
  - wear
    - causes
      - hardness
    - possible solutions
      - higher hardness
  - contamination
    - causes
      - coefficient of friction
    - possible solutions
      - plated surface
- solutions to current problems
    - higher grade material
      - A2 hardened steel
    - tighter tolerance machining
      - higher tolerance drawing
    - higher hardness
      - A2 hardened steel
    - plated surface
      - electro-less nickel coating